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SECTION 09 84 36   |   SOUND-ABSORBING CEILING UNITS
VET Acoustical Baffles

  PART 1   GENERAL
1.01	SECTION INCLUDES
A.	VET acoustical baffles suspended from ceilings or overhead structure to reduce reverberation and improve sound quality in large-volume spaces.
B.	Related Sections:
1.	Section 09 51 00: Acoustical Ceilings.
2.	Section 09 84 13: Fixed Sound-Absorptive Panels.
3.	Section 09 84 33: Sound-Absorbing Wall Units.
1.02	REFERENCES
A.	American Society for Testing and Materials (ASTM)
1.	ASTM C423: Standard Test Method for Sound Absorption and Sound Absorption Coefficients by the Reverberation Room Method.
2.	ASTM E795: Standard Practices for Mounting Test Specimens During Sound Absorption Tests.
3.	ASTM E84: Standard Test Method for Surface Burning Characteristics of Building Materials.
B.	UL Solutions (UL)
1.	UL 723: Standard for Test for Surface Burning Characteristics of Building Materials.
C.	National Fire Protection Association (NFPA)
1.	NFPA 701: Standard Methods of Fire Tests for Flame Propagation of Textiles and Films.
D.	International Code Council (ICC)
1.	ICC IBC: International Building Code.
1.03	SUBMITTALS
A.	Product Data: Manufacturer’s technical data for each type of acoustical baffle, including dimensions, core material, facing, mounting accessories, suspension hardware, and acoustical performance.
B.	Samples: Product sample and PVC facing color samples for selection, if applicable.
C.	Shop Drawings: Indicate baffle layout, suspension points, and coordination with lighting, sprinklers, HVAC, and other ceiling elements.
D.	Certificates:
1.	Flame spread and smoke development certification per ASTM E84 / UL 723.
2.	Sound absorption test results per ASTM C423 and ASTM E795.
1.04	QUALITY ASSURANCE
A.	Qualifications:
1.	Manufacturers: Minimum 5 years’ experience manufacturing acoustical baffles. Provide acoustical baffles from a single manufacturer.
2.	Installers: Qualified to perform work in accordance with manufacturer’s instructions.
B.	Performance Requirements:
1.	Surface Burning Characteristics: Acoustical baffles to perform as specified when tested in accordance with ASTM E84 / UL 723. Surface burning performance should comply with the International Building Code and other local building code requirements.
2.	Acoustical Characteristics: Acoustical baffles to perform as specified when tested in accordance with ASTM C423 and ASTM E795.
1.05	DELIVERY, STORAGE, AND HANDLING
A.	Deliver in unopened factory packaging with labels intact.
B.	Store indoors in a clean, dry space protected from moisture, direct sunlight, and physical damage.
1.06	SITE CONDITIONS
A.	Existing Conditions: Do not install baffles until the building is enclosed and HVAC systems are operational.
1.07	WARRANTY
A.	Provide manufacturer’s standard 1-year warranty against material defects per Section 01 77 00, Closeout Procedures.
  PART 2   PRODUCTS
2.01	MANUFACTURERS
A.	Manufacturer: NetWell Noise Control
10567 165th St. W, Ste 106, Lakeville, MN 55044
Telephone: 1-800-638-9355   |   Email: help@controlnoise.com
Web: www.controlnoise.com
2.02	DESCRIPTION
A.	Product: VET Baffles by NetWell Noise Control.
B.	Description: Acoustical baffle wrapped in PVC vinyl film and suspended vertically from ceiling structures.
C.	Construction:
1.	Core: 2” thick semi-rigid fiberglass, 2.0 lb/ft³ density.
2.	Facing: 5 mil PVC vinyl film, sonic-sealed on all edges.
3.	Weight: Approximately 0.33 lb/sq ft.
D.	Product Options:
1.	Baffle Size (Width x Height): [Standard size from table below] [Custom size: ______]
a.	Standard Sizes:
	Height
	Available Widths

	2’
	2’, 4’, 5’, 6’, 8’, 10’

	4’
	4’, 5’, 6’, 8’, 10’



b.	Custom sizes available on request.
2.	Orientation: [Portrait] [Landscape]
3.	Grommets: [Nickel-plated (standard)] [Stainless steel]
4.	Suspension: [NetWell Baffle Suspension Kit] [Chain] [Cable ties] [Wire] [Other ceiling-hung hardware]
E.	Product Performance:
1.	Acoustical Performance:
a.	Sound Absorption per ASTM C423 and ASTM E795, both faces exposed:
	Baffle Size
	Thickness
	Sabins per Baffle
	NRC Equivalent

	4’W x 2’H
	2”
	8.54
	1.07



2.	Surface Burning Performance:
a.	Fire Rating per ASTM E84 / UL 723: Class A.
b.	PVC Facing: Meets NFPA 701.
3.	Environmental:
a.	Contains no formaldehyde.
b.	Recyclable fiberglass core.
2.03	ACCESSORIES
A.	Grommets: Factory installed as specified. Number of grommets varies with baffle size and orientation.
B.	Suspension Kit (Optional): NetWell Baffle Suspension Kit, available from the baffle manufacturer. Provide one kit per grommet.
1.	Cable: 1.5 mm steel cable, 2 m (approximately 6’-6”) length.
2.	Ceiling Mount: Quick connect ceiling fitting, fastened to structure with a screw.
3.	Baffle Connection: Adjustable loop at cable end, sized by pressing the release button on the loop fitting, passed through the baffle grommet.
4.	Load Capacity: 25 kg (55 lb) maximum per kit.
C.	Other Suspension Hardware: Where the suspension kit is not used, provide suspension hardware by others, rated for the weight of the baffles and suitable for the ceiling structure.
  PART 3   EXECUTION
3.01	EXAMINATION
A.	Verification of Conditions:
1.	Verify that ceiling conditions and structural supports are suitable for baffle installation.
2.	Report unsatisfactory conditions to the General Contractor in writing.
3.02	INSTALLATION
A.	Install baffles per manufacturer’s installation instructions and approved shop drawings.
B.	Suspend baffles from ceiling structure using the NetWell Baffle Suspension Kit or another approved method such as chain, cable ties, or wire. Provide one suspension point at each grommet, and use fasteners suited to the ceiling structure.
C.	Hang baffles level, plumb, and evenly spaced for optimal acoustical and visual performance.
D.	Coordinate with lighting, sprinkler systems, HVAC, and other ceiling-mounted equipment, and maintain clearance from light fixtures and sprinkler heads.
3.03	CLEANING
A.	Clean baffles with a mild detergent and damp cloth. Do not use abrasive cleaners.
3.04	PROTECTION
A.	Protect installed products from damage until project completion.
END OF SECTION
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